## Slide 1: Characterizing electron-collecting CdTe for use in a 77 ns burst-rate imager
Lena Franklin
September 21, 2023
Lightbulb filament radiograph with e- CdTe detector
Notes: Look at other speakers too
Slide discussing depolarization

## Slide 2: Motivation: APS Upgrade
Advanced Photon Source (APS) at Argonne National Lab upgrading
  Reduced emittance, increased brightness
  154 ns to 77 ns bunch spacing
Once per bunch imaging requires new detectors
  Faster time-resolved experiments
  Applications: protein dynamics, materials science (shock physics, crack propagation), etc.
R. Hettel, "Status of the APS-U Project." 12th Int. Particle Acc. Conf. (2021).
Notes: Upgrades
Time resolved studies

## Slide 3: Single Bunch Imaging
Single bunch imaging example: diffraction patterns of metals under high strain rates
Husted et al, Rev. Sci. Intrum. (2018)

## Slide 4: Detector Goals
Goal: 77 ns burst x-ray imaging at 40 keV
  Fast electronics under development
  High-Z sensor material with fast charge collection
Simulations suggest 750 µm e- CdTe is fast enough
This talk: real-world sensor properties tested using pulsed laser and single x-ray bunches
Notes: 40+ keV
Detector requirements
Material and simulations
Talk summary

## Slide 5: Testing on Keck Pad Platform
Sensor: 750 µm e- Schottky CdTe from Acrorad
ASIC: Keck PAD – 8 frame burst imager, 128x128 150 µm pixels
  ASIC designed for 154 ns imaging
X-rays
Pixel array detector (PAD):
Semiconductor sensor bonded pixel-by-pixel to custom readout ASIC
From [3]
Storage capacitors
Integration capacitors
Modified from [4]
Pixel ASIC
Notes: Group developed many ASICs, one is KECK
KECK history and specs
detail on circuits: charge integration amplifier, selectable gain, etc.
New electronics

## Slide 6: Detector Speed and Induced Current
Detector speed limited by the duration of the current pulse
Goal: 90% of induced current in 35 ns
Electron collecting simulation
Current pulse < 50 ns
Hole collecting simulation
Current pulse > 200 ns
1/e length 40 keV = 90 µm
750 µm CdTe used due to availability
e-
e-
h+
h+
40 keV
150 keV
Lower energies are faster in e- CdTe
x-rays
x-rays
ASIC side
Notes: Can do two plots, one with both e and h to show differences
Mention that the total integral of the current needs to happen in ~35ns, could be helpful to show the integral
integrate + electronics in 77ns
35 ns for integration, 90% CC
Induced current due to holes + electrons, comment on speeds
Lower energies better in CdTe

## Slide 7: Measuring Induced Current
Detector triggered with variable delay from photon pulse
Integration window is "scanned" through induced current pulse
window 1
window 2
window 3
X-Ray Burst, Laser pulse, etc.
Current Pulse
Integration window
Notes: Need to understand induced current – but it happens faster than 100ns integration time
Soln: many images at different phases, can back out characteristics of the current

## Slide 8: Measuring Detector Speed
Result compared with MATLAB simulations
  Simulates induced current and integration process w/detector electronics
Charge collection time from rise/fall times of the curve
Simulation e- CdTe
40 keV photons, -400V bias, 200ns integration
Simulation of the induced current (top) and the result of scanning an integration window through
Notes: What this integrated curve looks like in practice
2 ways to study – rise/fall times, will look mostly at fall times in this prez
Compare with a simulation, describe

## Slide 9: Extracting Mobilities using Pulsed Optical Laser
Pulsed femtosecond laser generates e/h pairs in the sensor
Optical frequencies equated to x-ray energies by matching attenuation lengths
Extreme attenuation lengths used to study charge carrier mobilities
  515 nm: conversion near top of sensor, can extract electron mobility
  1030 nm: uniform conversion, can extract hole mobility from tail. Slowest case for detector behavior.
Laser & variable attenuation
Partially reflective mirror
Delay generator
Fast photodiode
Detector
Oscilloscope
Phase between laser pulse and beginning of integration measured on oscilloscope
Integration is triggered by previous pulse + a variable phase delay
Integration region >> sensor thickness
Notes: Early testing w/ optical laser – goal was to find electron hole mobilities
We need pulsed source for testing
Optical frequencies induce e/h pairs
Optical to x ray
In this test we use femtosecond laser (Explain setup)
Integration region >> thickness!
515 vs 1030nm

## Slide 10: Carrier Mobilities
Only holes contribute to the tail past ~35ns. Hole mobility around 100 ± 15 cm2/(V⋅s) at 0 C. Other sources report 80-110 cm2/(V⋅s) for CdTe.
Photons convert at the top of the sensor, signal is due to electrons. Electron mobility of 990 ± 100 cm2/(V⋅s) at 0C.
Other sources report 850-1100 cm2/(V⋅s) for CdTe.
The measured electron and hole mobilities agree within uncertainties to expected values for CdTe (see [5]).
Notes: 515, 1030
  1030 is worst case
Goal: appx value
Agree with expected, supports simulation

## Slide 11: Single bunch x-ray testing
X-ray testing at Cornell High Energy Synchrotron Source (CHESS)
Primary energy ~29.2 keV, attenuated beam used to study higher energy behavior
Periodic signal – e.g. synchrotron ring clock
KECK Pad
Delay generator for hardware triggering
Oscilloscope
Frame timing information
HW trigger
Bunch spacing ~280 ns
Bunch length ~83 ps
Notes: X rays important b/c fluorescence
CHESS @ cornell
Bunch spacing and triggering scheme
Energies used, sharing time

## Slide 12: 29.2 keV Testing
Scattered beam isolates 29.2 keV
e- CdTe requires <35 ns for 90% charge collection at 29.2 keV, –400V bias
X-ray fluorescence slows charge collection
  Cd K-α edge at 26.7 keV
29 keV photons convert at 1/e = 72 um
23 keV fluorescent photons create holes deeper in the detector, 1/e = 120 um
Main Beam
Aluminum Scatterer
Detector
Scattered Photons
Notes: Fluorescent photons have > atten length than primary
Scattered
X-ray fluorescence is bad
  At 29.2, Cd fluoresces
  Resolution, speed
Plot, effects of adding fluorescence
Still achieves timing requirements

## Slide 13: Higher Energy Testing
29.2 keV attenuated out of main beam, higher harmonics are used to study higher energy behavior
83% of signal occurs in 35 ns, 90%+ should be possible at 40 keV
Main Beam
Primary 29.2 +
Harmonics
5 mm steel
29.2 keV trans. ~10-16
Attenuated beam, mostly harmonics
Detector
Approximately
67% N=2→58.4 keV
20% N=3→87.6 keV
13% N=4→116.8 keV
Beam composition estimated from scattered photons
Notes: Beam composition estimated from spectra of scattered photons.
Labels on axes bigger, title B (for all plots), include voltage (go through whole presentation)
See if I can get a spectrum to show on slide
Attenuated out 29.2 keV
Used scatter to determine the beam composition
At these energies, 83% in 35 ns
At lower energy (faster behavior), 90% is possible
CONCLUSION: 750um CdTe is fast enough

## Slide 14: Sensor Polarization
Dosing leads to decreased sensitivity and uniformity
X-ray source: Al filtered Ag x-ray tube
Results similar to h+ CdTe (see [6]), polarization is slowed by
  Lower temperatures
  Higher bias voltages
Normalized Average Signal
Normalized Average Signal
Polarization and Temperature at –200 V
Polarization and Bias at 0 C
~1.3x1011 photons/mm2 dose in 1.5 hours
Notes: Cite hole collecting paper
Also need to understand polarization
Define
Also when biased for a long time
Setup (ag tube ect), flood illumination
Describe plots
Reference prev CdTe results, best operating conditions

## Slide 15: Polarization Flood Images (Preliminary Result)
h+ CdTe exhibited a network of lines after polarization
e- CdTe exhibits a line network and prominent bright spots with large signal amplitude
  More work needed to understand this
  h+ and e- from different batches, different Schottky barriers, taken at different times
Detector before and after ~1.3x1011 photons/mm2 at -200V
Previous results:
h+ CdTe
e- CdTe
Detector before and after ~3x1011 photons/mm2 at -200V
From [6]
Notes: Can look at them in grayscale, can check Julian’s folder for data (people and data)
Explain how average charge collected decreases with dosing, but in bright points local
What metals specifically? Check Acrorad literature, (Indium and Al?)
Preliminary results
These are examples of a flood illuminated image before and after dosing
In h+ CdTe the polarized image shows a network of lines
In e- CdTe the polarized image also shows a network of lines, but much more prominent are spots with high signal. These bright spots begin to appear before significant changes in the normalized average signal is visible.

## Slide 16: Radiographs
A line-pair mask
(numbers refer to # line pairs per mm)
Lightbulb filament
Object placed ~2 cm before detector
Raw images - no flatfield correction
Notes: Raw images w/ no flatfield correction
Some radiographs to give a qualitative indication that the sensor is able to be used for imaging
# lp per mm

## Slide 17: Conclusions
More work needed to understand polarization differences from h+ CdTe
750 µm e- CdTe is fast enough for 77 ns imaging at 40 keV
Acknowledgements
We thank the Department of Energy, the National Nuclear Security Administration (NNSA) and Argonne National Laboratory for their support.

## Slide 18: References
[1] R. Hettel, "Status of the APS-U Project." 12th Int. Particle Acc. Conf. (2021).
[2] Husted et al, "Time-resolved x-ray diffraction techniques for bulk polycrystalline materials under dynamic loading." Rev. Sci. Intrum. (2018)
[3] K. Shanks, "Development of photon-integrating area detectors for x-ray science." (Presentation, 2020)
[4] Kate Shanks "Detectors for high-speed imaging and diffraction at the Cornell High Energy Synchrotron Source." (Presentation, 2021)
[5] Suzuki et al, "Carrier Transport Properties of HPB CdZnTe and THM CdTe : Cl." IEEE Transactions on Nuclear Science. (2002)
[6] Becker et al, "Characterization of CdTe Sensors with Schottky Contacts Coupled to Charge-Integrating Pixel Array Detectors for X-Ray Science." JINST. (2016)