## Slide 1: HTS IDs developments at the ESRF
L. Bortot, F. Cianciosi, G. Le Bec, F. Perratone, Z. Qiu
May 15 – 16, 2026, Deauville, France

## Slide 2
Introduction HTS IDs Developments
Infrastructure and Tests Summary & Outlook

## Slide 3: Motivation: High-Field, Short-Period Undulators
Chart: Period (mm)
| 40 | 3.8 | 14 | 16 | 18 | 15 | 20 | 15.5 | 16
NbTi wire | 0.45 | 0.56 | 0.38 | 0.8 | 0.98 | 0.73 | 1.18 | 0.8 | 0.62
CPMU | 1.07 | 1.22 | 0.8926
Advantages
Higher Brilliance: Better spatial resolution, faster measurements, smaller samples
Higher harmonics: Expanded scientific capabilities on the same storage ring
Compactness: More space in straight sections, increased lattice flexibility
Accelerator Physic Perspective
More spectral brilliance
Higher photon energies
Keep high photon flux
Shorter higher
(1) Zhang, K., Calvi, M.. 2022 SUST 35 093001 (2) Benabderrahmane, C et al. doi:10.18429/JACoW-IPAC2022-THPOPT050
Figure: Planar undulators (various technologies)
Device
Chart: Period (mm)
| 8.8000000000000007 | 14 | 15 | 15 | 20 | 16 | 15.6 | 15.6 | 21 | 17 | 15.6 | 15
NbTi wire | 0.5 | 1.33 | 1.45 | 1.36 | 1.2 | 0.93 | 1.2 | 1.2 | 1.67 | 1.3 | 1.2 | 1.01
Nb3Sn wire | 1.83 | 1.2
ReBCO tape | 0.77 | 0.2
ReBCO bulk | 0.85 | 0.85 | 1.54
Model
Data from [1,2]
R&D Space
Notes: ONLY DEVICES
More power, not necessarily useful one
Power density B*dz
More periods -> brilliance
Short periods, higher energy - Check units font

## Slide 4: Currently Available Technologies (Industrial Scale)
Hypothesis: Permanent Magnets
PMUs / CPMUs constrained by material limit
Electromagnets
Doomed by Joule losses, ,
Superconducting magnets
DC Joule losses are abolished
HTS-ReBCO Tapes
Mature technology (~km of tapes)
Cryogen-free (no LHe)
Record-high engineering current density
  500 A/mm2 in a 2T field, at 60 K
  2000 A/mm2 in a 5T field, at 20 K
 Compact design (high power density)
Dilasser, G. PhD Dissertation, 2017
Notes: - Scaling factor: dimensions vs B field and gradient

## Slide 5: Potential Leap for Insertion Devices
Magnetostatics Simulations(1)
Planar undulator, simplified 2D geometry
Fusion grade(2), 65 um REBCO tape
Operations at 4.5 K, 80 % critical current
(1) see also https://indico.cern.ch/event/1326603/contributions/5773995/
(2) https://www.faradaygroup.com/en/product/
Vacoflux 50 yoke
Coil
In figure:
Is = 1000 A = 15 mm = 4mm
Unmatched HTS performance  Exploration of R&D space
Chart: Period (mm)
| 40 | 8.8000000000000007 | 8.8000000000000007 | 3.8 | 14 | 14 | 15 | 15 | 16 | 20 | 18 | 16 | 15 | 15.6 | 15.6 | 21 | 20 | 17 | 15.5 | 15.6 | 16 | 15
NbTi wire | 0.45 | 0.5 | 0.51 | 0.56 | 1.33 | 0.38 | 1.45 | 1.36 | 0.8 | 1.2 | 0.98 | 0.93 | 0.73 | 1.2 | 1.2 | 1.67 | 1.18 | 1.3 | 0.8 | 1.2 | 0.62 | 1.01
Nb3Sn wire | 1.83 | 1.2
ReBCO tape | 0.77 | 0.2
ReBCO bulk | 0.85 | 0.85 | 1.54
CPMU | 1.07 | 1.22 | 0.8926
Devices Models
Simulations
Potentially at reach!
Tech advance

## Slide 6: Technology challenges
Persistent Magnetization
Persistent eddy currents in superconductors, undesired contribution to principal magnetic field
Quench Phenomena
Local transition to the resistive state, Joule dissipation of stored energy
Mechanical Degradation
Brittle HTS layer, local defects, bending limits, delamination, Lorentz forces (static and transient phenomena)
Quench in the CFS-SPARC TF Coil(1)
(1) https://snf.ieeecsc.org/files/ieeecsc/ slides/LaBombard%20presentation.pdf
Possibly Irreversible degradation
Eddy currents in an HTS tape
Field quality degradation
Performance degradation
Tension (ab)
Tension (c)
Compression
Shear
Cleavage
Peel
Hideaki M., Yoshinori Y. IEEE 2014 4602412.
~50 MPa
>100 MPa
>20 MPa
~ 1 MPa
~ 1 MPa
~700 MPa

## Slide 7
Introduction HTS IDs Developments
Infrastructure and Tests Summary & Outlook

## Slide 8: A Superconducting Wiggler for BM18
BM18 Upgrade
field-tunable wiggler
low-photon-energy applications
tight space constraints (~250 mm length)
Principal Design Choices
Approach: simple, robust, modular
Iron-dominated electromagnet
80A, 1.58T @ 65K
Magnet vacuum separated from beam
Planar, double-pancake windings
No-insulation technique
High quench margin (~ 35%)
Demountable joints
Normal-conducting current leads
QF8
3PW
Flange
BPM
DQ2
Technological development platform towards short-period, HTS undulators
Maximize learning
Validate critical interfaces
De-risk details before they become failures

## Slide 9: Mechanical Assembly
Wiggler Assembly
Mechanical Forces
Central pole, beam-side winding Relevant radial forces
Pulse-tube cryocooler
Iron yoke
HTS
coil
Beam vacuum
chamber
Vacuum chamber
Current lead
Correction coil
Electrical feed-through
Detail: winding mandrel
102
168
2
62
127
61
2
76
53
Vectors in N Colormap in N/cm3
Upper | N | 40 | 260 | 40 | 5000
Lower | N | 450 | 1275 | 450 | 
beam
Forces management is crucial!

## Slide 10: Cryo-Electrical System
Layout
Conduction-cooled system
Electrically conducting mandrel
Aluminum nitride insulating interfaces
Bridge joints (Indium pressed, demountable)
Cryogenics unit
Pulse Tube, single-stage Cryocooler:
Less vibrations and maintenance than a GM
Only vertically oriented
Electrical insulation
Copper mandrel (winding support)
bridge connection
Cryo System
Winding
X2 safety factor @ 60K
Losses
Operation range
Open questions
Tunnel integration (utility lines)
Radiation hardness
Interfaces reliability!

## Slide 11: Quench and Beam Dynamics
Quench-Beam Interaction
Tape: quench initiation and propagation Winding: electro-thermal dynamics Coil: magnetic coupling
Simulations Nonlinear numerical problem: multi-physics, -scale , -rate (
No-Insulation Coils
Low turn-to-turn resistivity
Current redistribution during a quench
“Hot-spot” zone bypassed, reducing
Superconducting (left) and quenched (right)winding
+
-
+
-
Bypass current
Winding current
+
-
beam
Reliable and efficient simulations, how?

## Slide 12: Numerical Simulations
Magnetostatics
RADIA: the workhorse of the community
Exceptional for conventional ID geometries
Less flexible for non-symmetric designs
Magnetoquasistatics
FEA
Homogenized -form [1], 3D FEM code COMSOL
Verification: 2nd order -> slow, converged 1st order -> fast, not converged (so far)
Circuit model + Minimum EM entropy production
Turn-segment resolution Potential speedup (FMM compression) Careful element definition Nontrivial inductance matrix
winding orientation
[1] Mataira, R. C., et al. SuST 33.8 (2020): 08LT01.
Example: non-convex iron shape with round holes
Z. Qiu
Notes: Energy variation in a circuit subjected to KCL, voltages are lagrange multipliers associated to CKL constraint

## Slide 13
Introduction HTS IDs Developments
Infrastructure and Tests Summary & Outlook

## Slide 14: Coil Mechanical Considerations
Example: Small coil for short-period undulator (in mm):
Coil as stack of thin-walled cylinders (, )
Individual turn
hoop stress
normal pressure
Coil as stack of turns
Chart: Turn index (-)
Winding tension (N)
(*) estimated via SEM analysis and study of “fingerprints”
Usoskin, A., et al. IEEE Transactions on Applied Superconductivity 27.4 (2016): 1-5.
Tape cross-section
tape surface in mechanical contact
winding tension
geometry
Small radii, narrow tapes, many turns  minimize

## Slide 15: Winding Machine Procurement
Winding tests
HTS tape behavior at small radii ( 5-10 mm) In-house built winding machine
Experimental shape optimization
Excellent contact at tape-to-mandrel interface Reduced stress concentration in transitions
Design and Fabrication
2-12 mm tapes
610 to 250250 mm coil dimensions
1-10 N tension range with control
tape position accuracy mm
dual, independent payload for co-winding Low tape tension, tight control
Prototype
Winding machine
winding machine
Notes: CE compliant
Logo Automachine

## Slide 16: Prototype testing – 77K Liquid Nitrogen
Testing Philosophy
Learn robust current-controlled operation
Validate design principles for undulators
De-risk technology
Phase 1: 77 K Tests
Magnetic field mapping
Current-controlled scans  dynamic losses
Inter-turn resistance  current redistribution
Quench behavior  NI self-protection
Mechanical response
  Over-current regime
  Thermal cycles
  Quench transient
LN2 @ 77K
HTS coil
Power supply
Temperature monitoring
CTRL & DAQ
PC
Heater
Voltage monitoring
Conduction-cooled test bench for HTS coils
Hall Probe
bench
Quench detection
Quench protection

## Slide 17: Prototype testing – 60 K Cryocooler
Phase 2: 60 K Tests (Full Operation)
Full thermal characterization
  Mechanical assembly
  Cryocooler
  Current leads
  Joints
Magnetic field integral measurements
35% quench margin verification
Thermal cycling (10+ cycles)
  Windings assembly
  Demountable joints reliability
Mechanical response
  Lorentz forces
Power supply
Temperature monitoring
CTRL & DAQ
PC
Voltage monitoring
Conduction-cooled test bench for HTS coils
Undulator
bench
Quench detection
Quench protection
HTS wiggler
Vacuum pump
Pulse-tube Cryocooler
Notes: Undulator bench ( HALL probe + stretch wire)

## Slide 18
Introduction HTS IDs Developments
Infrastructure and Tests Summary & Outlook

## Slide 19: Summary and Outlook
Summary
HTS materials as key-enabling technology for high-field, short period undulators
Reliability and maintainability crucial aspects for adoption of HTS technology in light sources
HTS wiggler for BM18 upgrade as technological development platform
R&D program focused on bridging the gap between design and real operational reliability
Outlook
 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4
Coil design |  |  |  |  |  | 
REBCO tapes |  |  |  |  |  | 
Winding of prototype coil |  |  |  |  |  | 
Initial cold tests (LN2, 77 K) |  |  |  |  |  | 
Winding machine |  |  |  |  |  | 
Winding of magnet coil |  |  |  |  |  | 
Integration, tests (65 K) |  |  |  |  |  | 
2025
2026

## Slide 20
THANKS FOR YOUR ATTENTION
MANY THANKS TO
ESRF-IDM : C. Benabderrahmane, O. Benezech, F. Bidault, J. Caverot, B. Cottin, G. Giroud, M. Michel, L. Samaille, R. Versteegen
ESRF-ISDD: L. Eybert, F. Villard, B. Pelissier
ESRF-EXP-BM18: P. Tafforeau

## Slide 21
Backup slides

## Slide 22: Magnet Assembly

## Slide 23: Winding Machine Layout
Specifications
2-12 mm tapes
610 to 250250 mm coil dimensions
1-15 N tension range with control
tape position accuracy mm
dual, independent payload for co-winding
Low tension and tight control
Design and Fabrication (CE compliant)
Vertical alignment
Soldering station
Brushless motors
HMI
  Recipe system
  Data logging
  USB interface
ReBCO tape spool
Metal tape spool
Winding former
Prototype test, 26-02
Winding unit, 26-05

## Slide 24: Magnetic design
Magnetic flux density in the iron yoke. Holes for field quality optimization.
~ 65% of load line for operations at 65K First and second field integrals corrected
Magnetic flux density (top) and coil load line (bottom)
Beam angle, in mrad
Beam offset, in m

## Slide 25: HIGH-temperature superconducting TAPES
Critical surface (temperature, magnetic field, current density) for various superconductors.
(Amm2)
-
(T)
(K)
Materials superconducting above 77 K
Superconducting state below the critical surface, otherwise quench HTS-REBCO tapes
Copper oxides (CuO2) as thin films doped with rare earths, embedded in tapes.
Record-high critical current density
Critical temperature 93K (Nb-Ti: 9.2K)
Critical field 240T (Nb-Ti: 14.5T)
Anisotropic behavior (max. current density for to tape wide surface)
HTS performance > x10 than LTS !

## Slide 26: Commercially available superconductors
Considerations (some)
Physics: Temperature, magnetic field, current density, mechanical forces, radiation hardness…
Coil design: Shape, number of turns, layers and windings, joints, terminals …
Complexity: Power supply, vacuum system, cryogenic system, diagnostics …
Technology: Quality, characterization, data availability, reproducibility, quantity at industrial scale, supply chain resilience, price …
Liquid Helium
Liquid Nitrogen
REBCO tape
T
0
10
20
30
Low field
High field
Ultra High field
BSCCO 2212 wire
YBCO bulk
BSCCO 2223 tape
Nb-Ti wire
Nb3Sn wire
LTS
HTS
MgB2 wire

## Slide 27: technological Limits of REBCO TAPES (1/3)
Quench
Local transition from superconducting to normal conducting state
Stored magnetic energy  heat in the superconductor
Possible degradation due to local stress and thermal runaway
REBCO tapes:
High energy density
Slow quench propagation (high )  difficult quench detection  Potential damage
LHC accident (2008)
Quench in the CFS-SPARC TF Coil
Time
Hot spot
tape
Mitigate consequences of quench !
LaBombard IEEE-ASC 2024. https://snf.ieeecsc.org/files/ieeecsc/slides/LaBombard%20presentation.pdf

## Slide 28: magnetic field quality
Iron yoke shape optimized for minimizing field integrals
Optimization loop :
Model parameters
Model assembly
RADIA code (1) CPython C API (2)
https://github.com/ochubar/Radia
https://gitlab.esrf.fr/radia-esrf/radia-python
https://htsdb.wimbush.eu/dataset/25893079
Stochastic optimization
Multiprocessing on ESRF HPC cluster
Coil load-line
verification
Critical current measurement (3)
INIT
END
…